|  | PRESS RELEASE |
| --- | --- |

Child can get injured, strangulate or suffocate in bed ZBYSZEK P

(Prague, August 27, 2015) Officers of the Czech Trade Inspection Authority found out that a little bed made from pine wood is offered in the Czech market that poses serious safety risk to children users. Test proved low strength of used wooden parts which could result in injury of a child if sidewalls or bottom brake. Wholes and spaces in the bed can cause child’s injury if legs or arms or fingers get stuck in these spaces. Child can get caught on high corner edges with unsuitable clothing or decoration and subsequently strangulate. The bed was published in European database of dangerous products RAPEX, file number A12/1031/15.

Children’s bed ZBYSZEK P

Brief product description:	Classic timber bed made from pine wood

Product name:	 		ŁÓŻECZKO DZIECIECE „ZBYSZEK P“

Manufacturer:			WYTWÓRNIA MEBLI LESZEK WUJEC,

Other data:			Regon 250028476, NIP 621-003-13-98

Country of origin: 		Poland

Original product as assembled in test room

Danger

Laboratory test of material’s strength proved that within a usual and predictable way of use it is possible that a situation occurs when a child can get injured by damaged bed sidewalls or bottom after these parts brake as a result of insufficient strength of used timber parts. Dangerous wholes and spaces were also detected that could cause child’s injury in case when its legs, arms or fingers get stuck in these spaces.

Test also proved that the test chain’s loop catches on upper edge of all bed sides. In case that a child would get caught in the same way for example with a part of clothing or its decoration, it would strangulate.

It is not possible to absolutely exclude the risk of inhalation or swallowing a small spring which is accessible after a movable partitions slide on the sidewall is removed with the power of 44.8 N which can be used by a child under 3 years of age.

Conclusion

Classic timber bed is not in compliance with requirements of the Act No. 102/2001 Coll. on General Safety of Products. Numerous defects significantly influencing safety of the product were detected within tests carried out in compliance with applicable European standard EN 716-1/2:2008 + A1:2013).

Taken measures

Inspectorate of the Czech Trade Inspection Authority based in Pilsen imposed the final distributor a protective measure consisting of immediate recall of the product from distribution and withdrawal of the timber bed Zbyszek P from the consumer who purchased the dangerous product in the inspected workplace. Nowadays further investigation is carried out within distribution in the Czech Republic. All available documents and information concerning the dangerous children’s bed were handed over to a contact point of the RAPEX system at the Ministry of Industry and Trade and were published in the European database RAPEX, file number A12/1031/15.