|  | PRESS RELEASE |
| --- | --- |

CTIA: High content of water in diesel was an individual finding!

(Monitoring of fuels quality – February 2015)

(Prague, March 23, 2015) Monitoring and sampling of motor fuels continued in compliance with determined schedule in February. The plan was supplemented by investigation of consumers’ submissions. 3 of 236 collected samples failed quality requirements of technical standards. The most significant finding concerned water in one of diesel fuel samples – the water content exceeded the permitted amount of water almost 50 times. “This was the first time we detected such a case since 2001 when the Czech Trade Inspection Authority started monitoring fuels quality. Despite it was a technical defect and the particular vendor stopped selling the poor quality diesel, administrative proceedings will be launched,” said Mojmír Bezecný, the Director General of the Czech Trade Inspection Authority.

Samples of all monitored fuels, i.e. automotive petrol, diesel, diesel fuel blend, organic fuel, LPG, CNG, and Ethanol E85, were collected to inspections at filling stations on the whole territory of the Czech Republic.

Inspection results

In total 3 of 236 fuel samples failed determined quality requirements, i.e. 1.3%. Defects were detected concerning two samples of diesel and one sample of Ethanol E85.

Diesel

111 diesel fuel samples were collected and inspected. 2 of them failed quality requirements of applicable technical standard. In one case, the diesel sample failed quality parameter flash point. The measured value was 48.5%°C (minimal value is 53.0°C when measurement uncertainty is taken into account). In the other case, the inspected diesel fuel sample failed two quality parameters, namely appearance – presence of water. The measured value of 12,470 mg/kg significantly exceeded (by 48 times) the limit content of water as stipulated in the technical standard (maximal value is 260 mg/kg when measurement uncertainty is taken into account). Other inspected and analysed diesel fuel samples met requirements stipulated in the technical standard ČSN EN 590 – Motor Fuels – Diesel – Technical Requirements and Test Methods.

Ethanol E-85

Within the inspection of two samples of Ethanol E-85, CTIA detected noncompliant vapour pressure in one sample. The measured value of this parameter was 45.9 kPa and thus didn’t reach the minimal value as stipulated in the respective technical standard (i.e. 48.0 kPa when measurement uncertainty is taken into account). The other sample met the requirements of the standard ČSN P CEN/TS 15293 – Motor fuels – Ethanol E85 – Technical Requirements and Test Methods.

Organic ingredients in fuels

In February, content of fatty acid methyl ester was inspected in 111 diesel fuel samples and content of ethanol was inspected in 85 samples of automotive petrol. Laboratory analysis didn’t prove that the permitted content of organic ingredients was exceeded.

Conclusion

In February, the above mentioned results of inspections of fuel quality, i.e. shortcomings detected in 1.3% of collected and inspected samples, proved results of January when the rate of noncompliant samples was also 1.3%. Deviations from quality standards were detected concerning 2 diesel fuel samples and 1 sample of Ethanol E85. We saw improvement concerning diesel fuel, but the rate concerning Ethanol worsened. Inspections of fuels quality will continue in line with the schedule in March.

Výsledky podle inspektorátů:

Legenda: OD = odebráno, N = nevyhověl

Přílohy: 	Monitoring a sledování jakosti pohonných hmot únor 2015

Monitoring a sledování jakosti pohonných hmot leden-únor 2015