|  | PRESS RELEASE |
| --- | --- |

CTIA detected dangerous toys within international action

(Prague, February 6) The Czech Trade Inspection Authority took part in an international joint action aimed at inspecting toys. Seventeen European countries, including the Czech Republic, participated in the project. The inspections carried out within this international action were focused on plastic toys that could contain excessive amounts of some chemicals and pose a health risk to children. "This international audit confirmed the presumption that there are toys in the EU market that do not meet the safety requirements. During the inspections, the market surveillance was able to map and gather information and documents that could improve the situation in the EU internal market,” said the CTIA Director General Mojmír Bezecný.

The Czech Trade Inspection Authority participated in an international supervisory joint action aimed at inspecting the safety of plastic toys and unifying the attitude of the national inspection authorities to these products. Laboratory assessment of selected products by accredited laboratories was also a part of the project. Test laboratories examined the presence of different types of chemicals that can be used during the manufacturing process of these toys. In particular, the possible occurrence of substances such as phthalates (phthalic acid esters), SCCPs (PAHs) and BPA (bisphenol A) were investigated. Furthermore, the presence of selected chemical elements, such as cadmium, lead, and organic tin were also tested. All these elements can be very dangerous to the developing child's organism if their concentration in toys exceeds the limits set by the applicable legislation.

Seventeen European countries took part in the joint action. The total of 255 models of plastic toys were collected and inspected. All samples were tested for phthalate, SCCP, lead, cadmium, and organic tin content. A smaller number of toys were tested for PAH and BPA.

The Czech Trade Inspection Authority took in total 15 toys models, including 3 that were assessed as noncompliant due to the serious risk caused by the excessive amount of phthalates in the material used to manufacture the toys (phthalates are substances that interfere with fertility and can also increase the risk of allergies).

The Czech Trade Inspection Authority ordered the distributors of these toys to take protective measures consisting of prohibition of distribution of these products as well as the withdrawal of products from distribution.

We speak about the following dangerous toys that were published on the CTIA website and notified in the RAPEX system through the contact point and the Ministry of Industry and Trade.

For example, a large amount of phthalates were found in a plastic toy „Žlutá pískací žába“ ("Yellow Whistling Frog"). The limit permitted by valid legislation was exceeded by more than 400 times. In the toy, the following substance was detected in the following amount: DEHP = Bis (2-ethylhexyl) phthalate in the range of 48.0 ± 5.7% by weight, with the permitted limit being 0.1%.

ŽLUTÁ PÍSKACÍ ŽÁBA

Information about the product were published in RAPEX, notification number A12/0155/18

https://www.coi.cz/coi-stahuje-z-trhu-piskaci-zabu-kvuli-ftalatum/

NAFUKOVACÍ KLADIVO „DOIPHIN“

Information about the product were published in RAPEX, notification number A12/1585/17

https://www.coi.cz/i-hracka-do-vody-muze-byt-nebezpecna/

PANENKA FASHION GIRL

Information about the product were published in RAPEX, notification number A12/1634/17

https://www.coi.cz/nebezpecna-panenka/