|  | PRESS RELEASE |
| --- | --- |

Presented characteristics of four insulation products failed the reality

(Praha, December 9, 2019) The Czech Trade Inspection Authority evaluated the inspections focused on thermal insulation products for the building industry. These were industrially produced mineral wool products and polystyrene foam products. In total, it inspected 57 products and found 36 deficiencies. Although most errors were of a formal nature, tests carried out by an accredited laboratory showed that some polystyrene insulations don’t meet the manufacturer's declared characteristics.

The Czech Trade Inspection Authority carried out inspections of thermal insulation products for the construction industry, which, when placed on the market, should meet the requirements of the relevant regulation on construction products as well as harmonized standards. These are industrially manufactured products made of mineral wool or polystyrene foam, which are used for thermal insulation of buildings.

Within this nationwide project, CTIA officers carried out 49 inspections during which they inspected 57 products. Deficiencies were found in 36 cases. The most common were administrative errors regarding the CE marking; the CE marking of construction products must also contain other information set in the Regulation and a declaration of characteristics.

14 items of thermal insulation products were tested by an accredited laboratory, where 4 polystyrene insulations didn’t correspond to the characteristics declared by the manufacturer. These were, for example, the thermal conductivity coefficient or the water vapour permeability.

The Czech Trade Inspection Authority imposed on-the-spot fines amounting to CZK 60,000 for 7 inspected entities. Furthermore, 5 administrative proceedings were initiated.