|  | PRESS RELEASE |
| --- | --- |

The samples of tested AdBlue liquid passed in all parameters

(Prague, 2 December 2021) The Czech Trade Inspection Authority inspected the AdBlue liquid, which is used to run some diesel vehicles and is a necessary preparation for reducing harmful nitrogen oxide emissions. The CTIA carried out a total of 57 inspections, including 14 cases expert tests that were carried out by an accredited laboratory. The tested samples of AdBlue liquid passed all the tested parameters.

In the period from 1 March to 30 June 2021, the Czech Trade Inspection Authority carried out inspections focused on the quality of AdBlue and compliance with the obligations set out in Act No. 634/1992 Coll., on Consumer Protection, particularly on the labelling of these products. The inspected entities were physical and legal persons.

The inspectors carried out 57 inspections and inspected a total of 73 products. 14 samples of AdBlue were taken with the participation of the staff of an accredited testing laboratory and were offered directly from dispensers at petrol stations. The samples of AdBlue liquid taken and tested by the accredited testing laboratory passed all the tested parameters (density at 20°C, IR spectrum, refractive index at 20°C, urea content, mechanical impurities gravimetrically, alkalinity as NH3, biuret content, aldehyde content, phosphate content, elemental analysis - aluminium, chromium, copper, iron, nickel, potassium, sodium, calcium, magnesium, zinc, phosphorus).

Breaches of Act No. 634/1992 Coll., on Consumer Protection, were found during 6 inspections. These included, for example, the use of a volumetric meter without valid official verification at the distribution pump of the dispenser when selling AdBlue. In another case, the Czech text concerning the minimum durability (lifetime) of the product was missing and only foreign language text was available.

The Czech Trade Inspection Authority imposed 3 fines for the above-mentioned infringements, totalling CZK 5,500.