|  | PRESS RELEASE |
| --- | --- |

Seal with balloon contained too much lead, CTIA ordered recall

(Prague, 22 September 2022) The Czech Trade Inspection Authority has found that a product in the domestic market poses a serious risk. It is a battery-operated toy seal with balloon, model NO. LD - 128A.

The Czech Trade Inspection Authority has detected a dangerous 3 x 1.5 V battery-operated toy in the shape of a seal with a balloon in the market, the material of the toy is plastic and metal. The toy is packed in a paper box with the following information. The toy is not suitable for children under 3 years of age.

The testing laboratory has confirmed significant non-compliance with the requirements of Government Regulation No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment (Directive 2011/65/EU - RoHS). The solder joint inside the toy was found to have a lead content exceeding the permitted limit value of 0.1% by a factor of up to 68.9%. Failure to comply with the requirements of the current legislation poses a serious environmental risk due to potential environmental pollution. Furthermore, the CTIA found that the product was not provided with complete identification of the manufacturer and importer and that other information and warnings were not provided in the Czech language, thus the product does not meet the requirements of Government Regulation No. 86/2011 Coll., on Technical Requirements for Toys.

The Czech Trade Inspection Authority, in order to prevent further occurrence of identical products in the market, imposed a protective measure on the distributor (Article 18a(4) of Act No. 22/1997 Coll., on Technical Requirements for Products), which is to withdraw the above-mentioned product from the market. The product was reported to the Safety Gate system for the rapid exchange of information on dangerous non-food products.

Product information:

Hračka na baterie „Stunt Sea Lion“

Trademark: 				DIDAI

Model number: 	NO.LD.-128A

EAN:					5961177000000

Production serie number:		not provided

Manufacturer:				MADE IN CHINA

Importer:	not provided

Product origin:			              China