|  | PRESS RELEASE |
| --- | --- |

The train contained too much lead, the CTIA ordered a recall

(Prague, 26 September 2022) The Czech Trade Inspection Authority has found that a toy on the domestic market is dangerous. It is a battery-powered train that has a lead content on the soldered joint inside the toy far much higher than the maximum permitted by legal regulations.

The Czech Trade Inspection Authority has detected a 2 AA batteries toy train for children in the domestic market, which consists of two cars and two trains. The product is packaged in transparent plastic packaging with a paper backing, where there is an illustration for inserting the batteries with instructions in Chinese characters. The toy is not suitable for children under 36 months.

The testing laboratory confirmed that the solder joint inside the toy had multiple exceedances of the lead content up to 62.5% when the permitted limit is 0.1% and the cadmium content up to 0.0799% when the permitted limit is 0.01% according to Government Regulation No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment (Directive 2011/65/EU - RoHS). The failure to comply with the requirements of the applicable legislation poses a serious environmental risk due to potential pollution. Furthermore, the product did not have the CE marking, did not have complete identification of the manufacturer and importer and was not accompanied by other prescribed information and warnings in the Czech language. Thus, the product does not meet the requirements of Government Regulation No 86/2011 Coll., on Technical Requirements for Toys.

The Czech Trade Inspection Authority has imposed a measure on the distributor (Article 18a(4) of Act No. 22/1997 Coll., on Technical Requirements for Products), which is to withdraw the above-mentioned product from the market. The toy was reported to the Safety Gate system for the rapid exchange of information on dangerous non-food products.

Product information:

Hračka na baterie „Vláček“ (Battery toy „Train“)

Trademark: 				CRH

Model number:				not provided

Production serie number:		not provided

EAN:					obal, hračka

Manufacturer:				not provided

Importer:				not provided

Distributor:				HQ SANG s.r.o., Spáčilova 1257/2, 618 00 Brno

DHH comfort s.r.o., Černovičky 1386/26, 627 00 Brno

Country of origin:				Čína

Bar code:				20000048572