|  | PRESS RELEASE |
| --- | --- |

CTIA bans battery-operated toy bee due to lead

(Prague, 18 January 2023) The Czech Trade Inspection Authority found that a product in the internal market poses a serious environmental risk. It is a bee-shaped battery-powered toy, model number 2152B.

The Czech Trade Inspection Authority detected a dangerous battery-operated toy in the shape of a bee in the domestic market. The toy is packed in a paper box with a plastic see-through window, which bears information and the CE marking. The toy is not suitable for children under 3 years of age. The material is plastic and metal.

Tests carried out by a qualified laboratory confirmed that the soldered joint inside the toy has a lead content exceeding the permitted limit of 0.1 % many times over, up to 46.7 %. Failure to comply with the requirements of the legislation in force (Government Regulation No 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment - Directive 2011/65/EU - RoHS) poses a serious environmental risk due to possible environmental pollution.

In addition, the product was not accompanied by information and safety instructions in the Czech language, but only in foreign languages (non-compliance with the requirements of Regulation No. 86/2011 Coll., on Technical Requirements for Toys). The product was also not accompanied by an indication of the maximum radio frequency power emitted in the frequency band in which the radio equipment is operated (required by Article 6(2)(b) of Government Regulation No. 426/2016 Coll. on the assessment of conformity of radio equipment when it is placed on the market).

The Czech Trade has imposed a ban on the distributor and a withdrawal of the product from the market or from circulation. The product was reported to the contact point at the Ministry of Industry and Trade and information about it was published in the Safety Gate system.

Product information:

Trademark: 				not displayed

Model number: 			2152B

Production serie number:		not displayed

EAN:					5902230135734

Manufacturer:					Shantou Create Toys Industrial Co., Ltd, 1-2 Floor,

6 Buldingg Guanghua Industry Area, Chengliang Road, Chenghal, District, Shantou City, China

Importer:	VENE POINT, ul. Lwowska 146A, 22-300 Krasnystaw, Polska